- Supporting Information -

Structural and magnetic properties of NiCx and NiNx (x = 0 to 1/3) solid solutions from first-principles calculations

C.M. Fang, M.H.F. Sluiter,  M.A. van Huis, H.W. Zandbergen

Table S1. Calculated dimensions of the calculation supercells for dilute C/N atoms in fcc and hcp lattices with C/N atoms at octahedral sites. The corresponding structures are displayed in Fig.  S1.

| figure Composition | lattice/stacking | Parameters (Å) |
| --- | --- | --- |
| S-1c) Ni32C | fcc/ | a = 7.097 |
| S-1c) Ni32N | fcc/ | a = 7.489 |
| S-1a) Ni54C | hex_fcc/abcabc | a = 7.505 c = 12.261 |
| S-1a) Ni54N | hex_fcc/abcabc | a = 7.506 c = 12.261 |
| S-1b) Ni54C | hcp/ababab | a = 7.489 c = 12.346 |
| S-1b) Ni54N | hcp/ababab | a = 7.489 c = 12.346 |
| S-1f) Ni32C2 | Fcc (C far away from each other) | a = 7.142 |

Table S2. Calculated local electronic configurations (EC, electrons), local magnetic configuration (MC, μB), and total magnetic moments (M, μB) at the Ni sites as nearest neighbors (NN, shell_1), and the next nearest neighbors (NNN, shell_2). The results for pure fcc-Ni metal are included for the sake of comparison.

| Ni sites | Ni32C | Ni32N |
| --- | --- | --- |
| Shell_1 X-6Ni | EC: 4s0.565 4p0.685 3d8.534 MC: 4s-0.01 4p-0.02 3d0.25 Moment: 0.23 | EC: 4s0.549 4p0.669 3d8.513 MC: 4s-0.01 4p-0.02 3d0.24 Moment: 0.22 |
| Shell_2 X-8Ni | EC: 4s0.552 4p0.584 3d8.468 MC: 4s-0.01 4p-0.02 3d0.64 M: 0.61 | EC: 4s0.552 4p0.582 3d8.468 MC: 4s-0.01 4p-0.02 3d0.66 M: 0.63 |
| pure fcc-Ni | EC: 4s0.566 4p0.609 3d8.464 MC: 4s-0.01 4p-0.03 3d0.67 Moment: 0.63 |

Supplementary Figure S1 (a-i): Schematics of supercells used for different NiXy (X = C/N) phases. The blue spheres represent Ni atoms, the green spheres C/N atoms.

Figure S1a: hex_fcc/abcabc_Ni54X                    Figure S1b: hcp/ababab_Ni54X

Figure S1c: fcc-Ni32X_oct                                            Figure S1d: fcc-Ni2X_tetra

Figure S1e: fcc-Ni32X2_close                               Figure S1f:  fcc-Ni32X2_far

Figure S1g: fcc-Ni32X4 (Ni8X)                          Figure S1h: fcc-N i32X8 (Ni4X)

Figure S1i: hcp-Ni24X9,  Striped green indicates C atoms at b sites