-  Supplementary Information -

Structural tale of two novel (Cr,Mn)C carbides in steel

G. K. Tirumalasetty, C.M. Fang, J. Jansen, T. Yokosawa, M.F.J. Boeije,

J. Sietsma, M.A. van Huis, H.W. Zandbergen

Table S.1: Nanobeam electron diffraction data used for the refinement of O- carbides using Model B and Model C in Table S2.

| MSLS - Model B |
| --- |
| Data set No | Zone | Number of observed reflections | Thickness (Å) | Crystal misorientation | R- value (%) |
|  |  |  |  | h | k | l |  |
| 1 | [201] | 148 | 379.8(13) | 0.010(17) | 0.006(11) | -0.021(3) | 2.737 |
| 2 | [102] | 155 | 134.5(15) | 0.052(3) | 0.15(3) | -0.026(5) | 4.151 |
| 3 | [110] | 249 | 466.4(16) | 0.163(3) | -0.163(3) | -0.012(4) | 7.006 |
| 4 | [102] | 127 | 136.9(12) | -0.186(12) | -0.02(3) | 0.093(6) | 9.045 |
| 5 | [102] | 103 | 130.6(13) | -0.08(11) | 0.13(3) | 0.044(6) | 3.160 |
| 6 | [100] | 148 | 377.5(3) | 0.00 | -0.302(8) | -0.05(10) | 4.496 |
| 7 | [201] | 131 | 380.6(13) | -0.013(18) | -0.020(11) | 0.027(4) | 2.767 |
| 8 | [102] | 160 | 135.4(13) | 0.044(10) | 0.20(3) | -0.022(5) | 4.791 |
| 9 | [210] | 177 | 168.0(12) | 0.266(11) | -0.53(2) | 0.565(14) | 8.024 |
| 10 | [102] | 124 | 130.0(14) | -0.086(11) | -0.12(3) | 0.043(6) | 3.043 |
| 11 | [210] | 186 | 193.1(19) | -0.133(8) | 0.266(17) | -0.462(14) | 8.430 |
| 12 | [010] | 227 | 239.4(4) | 0.151(17) | 0.000000 | 0.023(8) | 5.377 |
| 13 | [010] | 263 | 240.0(3) | -0.145(17) | 0.000000 | -0.014(8) | 4.664 |

| MSLS - Model C |
| --- |
| Data set No | Zone | Number of observed reflections | Thickness (Å) | Crystal misorientation | R- value (%) |
|  |  |  |  | h | k | l |  |
| 1 | [201] | 148 | 381.4(14) | 0.011(18) | -0.004(11) | -0.024(4) | 2.037 |
| 2 | [102] | 155 | 139.1(12) | 0.049(10) | 0.13(3) | -0.025(5) | 3.886 |
| 3 | [110] | 249 | 486.6(10) | 0.145( 3) | -0.145(3) | -0.011(4) | 8.249 |
| 4 | [102] | 127 | 141.8(12) | -0.180(11) | -0.02(3) | 0.090(6) | 9.064 |
| 5 | [102] | 103 | 134.4(14) | -0.084(11) | -0.13(3) | 0.042(5) | 3.154 |
| 6 | [100] | 148 | 394.4(6) | 0.000000 | 0.021(8) | 0.039(9) | 3.590 |
| 7 | [201] | 131 | 382.4(14) | -0.014(18) | -0.019(11) | 0.030(4) | 2.026 |
| 8 | [102] | 160 | 140.2(12) | 0.041(10) | 0.17(3) | -0.021(5) | 4.622 |
| 9 | [210] | 177 | 167.3(15) | 0.277(10) | -0.553(20) | 0.579(14) | 7.962 |
| 10 | [102] | 124 | 133.4(14) | -0.083(11) | -0.11(3) | 0.041(6) | 3.066 |
| 11 | [210] | 186 | 191.6(15) | -0.126(8) | 0.251(16) | -0.432(13) | 8.673 |
| 12 | [010] | 227 | 234.3(7) | 0.102(18) | 0.000000 | 0.021(8) | 4.210 |
| 13 | [010] | 263 | 234.6(7) | -0.099(18) | 0.000000 | -0.012(8) | 3.242 |

Table S.2: MSLS-refined structural parameters of O-carbide with Models B and C.

| MSLS - Model B |
| --- |
| Atomic Coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4c | 0.0688( 4) | 1/4 | 0.8289( 3) | 0.508(18) | 1.0 |
| Mn2 | 8d | 0.1945( 5)* | 0.0914( 3)* | 0.3468( 3)* | 0.383( 7)* | 0.5* |
| Cr1 | 8d | 0.1945( 5) | 0.0914( 3) | 0.3468( 3) | 0.383( 7) | 0.5 |
| C1 | 4c | 0.806( 3) | 1/4 | 0.4294(18) | 0.1 | 0.63( 4) |
| C2 | 4a | 0 | 0 | 0 | 0.1 | 0.062( 8) |

Space group: Pnma, a(O) = 5.09 Å, b(O) = 6.98 Å, c(O) = 4.55 Å,  α = β = γ = 90°, R = 5.28%. The temperature factor of C1 and C2 was set to 0.1, since the occupancy and temperature factor of an atom (in this case C1 and C2) are generally strongly coupled in the refinement. The * indicates the constraints used in the refinement procedure: x(Mn2) = x(Cr1), y(Mn2) = y(Cr1), z(Mn2) = z(Cr1), B(Mn2) = B(Cr1), Occ(Mn2) = 1- Occ(Cr1).

| MSLS - Model C |
| --- |
| Atomic Coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4c | 0.0711( 4)* | 1/4* | 0.8274( 3)* | 0.683(17)* | 0.6666667* |
| Cr1 | 4c | 0.0711( 4) | 1/4 | 0.8274( 3) | 0.683(17) | 0.3333333 |
| Mn2 | 8d | 0.1965( 5) | 0.0924( 3) | 0.3473( 2) | 0.386( 7) | 0.6666667 |
| Cr2 | 8d | 0.1965( 5)* | 0.0924( 3)* | 0.3473( 2)* | 0.386( 7)* | 0.3333333* |
| C1 | 4c | 0.810( 3) | 1/4 | 0.4571(17) | 0.1 | 0.796( 4) |
| C2 | 4a | 0 | 0 | 0 | 0.1 | 0.108( 8) |

Space group: Pnma, a(O) = 5.09 Å, b(O) = 6.98 Å, c(O) = 4.55 Å,  α = β = γ = 90°, R = 5.07%. The temperature factor of C1 and C2 was set to 0.1, since the occupancy and temperature factor of an atom (in this case C1 and C2) are generally strongly coupled in the refinement. The * indicates the constraints used in the refinement procedure: x(Mn1) = x(Cr1), y(Mn1) = y(Cr1), z(Mn1) = z(Cr1), x(Cr2) = x(Mn2), y(Cr2) = y(Mn2), z(Cr2) = z(Mn2), B(Mn1) = B(Cr1), B(Cr2) = B(Mn2),  Occ(Mn1) = 1- Occ(Cr1), Occ(Cr2) = 1- Occ(Mn2).

Table S.3: Nanobeam electron diffraction data used for the refinement of M- carbides using Model A and Model B in Table S4.

| MSLS - Model A |
| --- |
| Data set No | Zone | Number of observed reflections | Thickness (Å) | Crystal misorientation | R- value (%) |
|  |  |  |  | h | k | l |  |
| 1 | [100] | 240 | 240.3(10) | 0.000000 | 0.01( 3) | 0.014(10) | 5.083 |
| 2 | [100] | 240 | 240.0(10) | 0.000000 | -0.06( 3) | -0.003(10) | 5.302 |
| 3 | [201] | 150 | 204.1(13) | 0.008( 3) | 0.091(18) | -0.016( 5) | 3.539 |
| 4 | [201] | 143 | 212.3(12) | -0.035( 4) | -0.845(20) | 0.070( 8) | 8.999 |
| 5 | [201] | 172 | 155.6(20) | 0.314(11) | 0.83( 4) | -0.63( 2) | 3.067 |
| 6 | [100] | 233 | 236.6(11) | 0.000000 | 0.09( 3) | -0.015(10) | 8.095 |
| 7 | [100] | 255 | 240.2(10) | 0.000000 | 0.08( 3) | 0.057(10) | 8.219 |
| 8 | [201] | 138 | 211.3(12) | 0.053( 3) | -0.643(18) | -0.105( 6) | 3.695 |
| 9 | [201] | 135 | 268.7(17) | -0.185( 3) | -0.411(10) | 0.369( 6) | 1.733 |
| 10 | [100] | 222 | 237.7(10) | 0.000000 | -0.09( 3) | -0.029(10) | 8.450 |
| 11 | [100] | 262 | 238.9(11) | 0.000000 | -0.03( 3) | 0.070(11) | 8.457 |
| 12 | [100] | 242 | 240.2(10) | 0.000000 | 0.08( 3) | 0.060(10) | 7.202 |
| 13 | [203] | 97 | 238.2( 4) | 0.028( 3) | -0.117(18) | -0.018(20) | 4.483 |
| 14 | [203] | 95 | 240.2( 4) | 0.016( 3) | -0.179(14) | -0.010(19) | 6.240 |
| 15 | [203] | 84 | 234.2( 4) | -0.002( 3) | -0.032(19) | 0.002( 2) | 3.051 |
| 16 | [203] | 92 | 248.8( 5) | -0.023( 3) | 0.309(10) | 0.016( 2) | 6.522 |
| 17 | [203] | 90 | 244.3( 4) | 0.013( 3) | 0.173(13) | -0.008(19) | 6.295 |
| 18 | [203] | 90 | 243.5( 4) | 0.031( 3) | -0.223(12) | -0.020(20) | 4.947 |
| 19 | [203] | 90 | 242.9( 4) | -0.011( 3) | 0.147(16) | 0.007( 2) | 6.012 |

| MSLS - Model B |
| --- |
| Data set No | Zone | Number of observed reflections | Thickness (Å) | Crystal misorientation | R- value (%) |
|  |  |  |  | h | k | l |  |
| 1 | [100] | 240 | 234.5(10) | 0.000000 | 0.11( 3) | 0.013( 9) | 4.826 |
| 2 | [100] | 240 | 233.3(10) | 0.000000 | -0.08( 3) | -0.002( 9) | 5.208 |
| 3 | [201] | 150 | 200.9(13) | 0.008( 3) | 0.096(20) | -0.016( 5) | 3.777 |
| 4 | [201] | 143 | 213.9(11) | -0.034( 4) | -0.870(17) | 0.068( 7) | 7.906 |
| 5 | [201] | 172 | 158.7(20) | 0.315(11) | 0.83( 3) | -0.63( 2) | 3.089 |
| 6 | [100] | 233 | 230.0(10) | 0.000000 | 0.19( 3) | -0.019(10) | 7.923 |
| 7 | [100] | 255 | 233.4(10) | 0.000000 | 0.03( 4) | 0.053(10) | 8.739 |
| 8 | [201] | 138 | 212.0(11) | 0.053( 3) | -0.680(16) | -0.106( 6) | 3.369 |
| 9 | [201] | 135 | 263.3(17) | -0.180( 3) | -0.451(10) | 0.361( 6) | 1.845 |
| 10 | [100] | 222 | 230.6(10) | 0.000000 | -0.07( 3) | -0.032( 9) | 8.710 |
| 11 | [100] | 262 | 235.6(11) | 0.000000 | -0.25( 3) | 0.073(10) | 7.880 |
| 12 | [100] | 242 | 233.5(10) | 0.000000 | 0.02( 4) | 0.056(10) | 7.687 |
| 13 | [203] | 97 | 231.9( 3) | 0.025( 3) | -0.238(16) | -0.016(19) | 4.525 |
| 14 | [203] | 95 | 233.7( 3) | 0.013( 3) | -0.280(12) | -0.008(18) | 6.210 |
| 15 | [203] | 84 | 227.9( 3) | -0.004( 3) | -0.09( 2) | 0.002( 2) | 2.882 |
| 16 | [203] | 92 | 241.7( 5) | -0.021( 3) | 0.399( 9) | 0.014(20) | 6.579 |
| 17 | [203] | 90 | 237.4( 4) | 0.011( 3) | 0.270(12) | -0.007(18) | 6.089 |
| 18 | [203] | 90 | 236.7( 4) | 0.028( 3) | -0.326(10) | -0.018(19) | 5.037 |
| 19 | [203] | 90 | 236.2( 4) | -0.011( 3) | 0.238(15) | 0.007(19) | 5.782 |

Table S.4: MSLS-refined parameters of M-carbide with Models A and B.

| MSLS – Model A |
| --- |
| Atomic coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4e | 0.102( 3) | 0.3194( 9) | 0.1334(14) | 0.1 | 0.75 |
| Cr1 | 4e | 0.102( 3)* | 0.3194( 9)* | 0.1334(14)* | 0.1* | 0.25* |
| Mn2 | 4e | 0.430( 3)* | 0.3742( 6)* | 0.1528(17)* | 0.71( 7)* | 0.75* |
| Cr2 | 4e | 0.430( 3) | 0.3742( 6) | 0.1528(17) | 0.71( 7) | 0.25 |
| Cr3 | 4e | 0.2414(10) | 0.8573( 7) | 0.0091(15) | 0.81( 7) | 1.0 |
| C1 | 4e | 0.299( 2) | 0.4423(16) | 0.884( 2) | 3.2( 4) | 1.0 |
| C2 | 2a | 0 | 0 | 0 | 0.1 | 1.0 |

Space group: P21/c, a(M) = 6.83 Å, b(M) = 4.54 Å, c(M) = 5.00 Å,  α = γ = 90°, β(M) = 92.2°, R = 5.03%. The temperature factor of Mn1, Cr2, C2 was set to 0.1, since the occupancy and temperature factor of an atom (in this case Mn1, Cr2, C2) are generally strongly coupled in the refinement. The * indicates the constraints used in the refinement procedure: x(Cr1) = x(Mn1), y(Cr1) = y(Mn1), z(Cr1) = z(Mn1), x(Mn2) = x(Cr2), y(Mn2) = y(Cr2), z(Mn2) = z(Cr2), B(Cr1) = B(Mn1), B(Mn2) = B(Cr2), Occ(Cr1) = 1- Occ(Mn1), Occ(Mn2) = 1- Occ(Cr2)

| MSLS – Model B |
| --- |
| Atomic coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4e | 0.103( 2) | 0.3220( 7) | 0.1327(13) | 0.1 | 0.5 |
| Cr1 | 4e | 0.103( 2)* | 0.3220( 7)* | 0.1327(13)* | 0.1* | 0.5* |
| Mn2 | 4e | 0.4311(16)* | 0.3731( 5)* | 0.1534(13)* | 0.19( 5)* | 0.5* |
| Cr2 | 4e | 0.4311(16) | 0.3731( 5) | 0.1534(13) | 0.19( 5) | 0.5 |
| Mn3 | 4e | 0.2533( 8)* | 0.8539( 6)* | 0.0160(12)* | 0.50( 4)* | 0.5 |
| Cr3 | 4e | 0.2533( 8) | 0.8539( 6) | 0.0160(12) | 0.50( 4) | 0.5 |
| C1 | 4e | 0.306( 2) | 0.4464(16) | 1.8( 2) | 0.887( 2) | 1.0 |
| C2 | 2a | 0 | 0 | 0 | 0.1 | 1.0 |

Space group: P21/c, a(M) = 6.83 Å, b(M) = 4.54 Å, c(M) = 5.00 Å,  α = γ = 90°, β(M) = 92.2°, R = 4.96%. The temperature factor of Mn1, C2 was set to 0.1, since the occupancy and temperature factor of an atom (in this case Mn1, C2) are generally strongly coupled in the refinement. The * indicates the constraints used in the refinement procedure: x(Cr1) = x(Mn1), y(Cr1) = y(Mn1), z(Cr1) = z(Mn1), x(Mn2) = x(Cr2), y(Mn2) = y(Cr2), z(Mn2) = z(Cr2), x(Mn3) = x(Cr3), y(Mn3) = y(Cr3), z(Mn3) = z(Cr3), B(Cr1) = B(Mn1), B(Mn2) = B(Cr2), B(Mn3) = B(Cr3), Occ(Cr1) = 1- Occ(Mn1), Occ(Mn2) = 1- Occ(Cr2), Occ(Mn3) = 1- Occ(Cr3).

Table S.5: Calculated lattice parameters and formation energies for binary chemical composition of L3C1+x (L= Cr and Mn; x = 0, 0.25) and ternary composition (Mn2Cr)C1+x (x = 0, 0.25) 
ΔE = {E(Ln1Ln2Cm) – [n1 Eelem(Ln1)+n2 Eelem(Ln2) + m E(C)]}/ (n1+n2+m) is the formation energy with respect to the elemental solids (Bcc-Mn/Cr, graphite).

| Compound | Atom | Wyckoff site | DFT-GGA | Experimental | ΔE |
| --- | --- | --- | --- | --- | --- |
| Mn3C | Mn1 | 8d | a = 4.934 b = 6.671 c = 4.443 | a = 5.080 b = 6.772 [16] c = 4.530 | -211.5 |
|  | Mn2 | 4c |  |  |  |
|  | C1 | 4c |  |  |  |
| Cr3C | Cr1 | 8d | a = 5.194 b = 6.628 c = 4.509 | a = 5.033 b = 6.731 [12] c = 4.483 | -108.0 |
|  | Cr2 | 4c |  |  |  |
|  | C1 | 4c |  |  |  |
| Mn2CrC | Mn1 | 8d | a = 4.995 b = 6.762 c = 4.415 | No data available | -188.8 |
|  | Cr1 | 4c |  |  |  |
|  | C1 | 4c |  |  |  |
|  | Mn1 | 8d | a = 4.997 b = 6.667 c = 4.487 |  | -190.1 |
|  | Mn2 | 4c |  |  |  |
|  | Cr1 | 8d |  |  |  |
|  | C1 | 4c |  |  |  |
|  | Mn1 | 4c | a = 5.001 b = 6.709 c = 4.412 |  | -183.4 |
|  | Mn2 | 8d |  |  |  |
|  | Cr1 | 8d |  |  |  |
|  | Cr2 | 4c |  |  |  |
|  | C1 | 4c |  |  |  |
| Mn3C1.25 | Mn1 | 8d | a = 5.047 b = 6.953 c = 4.519 |  | -162.7 |
|  | Mn2 | 4c |  |  |  |
|  | C1 | 4c |  |  |  |
|  | C2 | 4a |  |  |  |
| Cr3C1.25 | Cr1 | 8d | a = 5.138 b = 6.878 c = 4.613 |  | -93.7 |
|  | Cr2 | 4c |  |  |  |
|  | C1 | 4c |  |  |  |
|  | C2 | 4a |  |  |  |

Table S.6: The DFT-GGA results for the replacements of Fe in the O-carbide. ΔE (eV/C) is the energy of adding one C at 4a sites of cementite-phase (L3C1 to L3C1.25).

| Phases | Lattice Parameter (Å) | ΔE (eV/C) |
| --- | --- | --- |
| Fe3C1.25 | a = 5.011 b = 6.940 c = 4.578 | 0.517 |
| Mn3C1.25 | a = 5.047 b = 6.954 c = 4.519 | 0.618 |
| Cr3C1.25 | a = 5.138 b = 6.878 c = 4.613 | 0.135 |
| (Mn2/3Cr1/3)3C1.25 | a = 5.032 b = 6.959 c = 4.526 | 0.650 |

Table S.7: The DFT-GGA results for the replacements of Fe in the M-carbide.

| Phases | Lattice Parameter (Å) | ΔE (eV/f.u.) |
| --- | --- | --- |
| (Mn1/2Cr1/2)3C1.5 | a = 5.067 b = 7.124 c = 4.576 β = 88.7 ° | 0.00 |
| (Fe1/3Mn1/3Cr1/3)3C1.5 | a = 5.083 b = 7.007 c = 4.569 β = 88.7 ° | 0.205 |
| (Fe2/3Mn1/6Cr1/6)3C1.5 | a = 5.040 b = 7.078 c = 4.645 β = 87.8 ° | 0.237 |

Table S.8: Comparison of experimental crystal structure information of the O-carbide with DFT Models A, B and C.

| DFT - Model A |
| --- |
| Space group | Pnma (nr. 62) |  |  |  |  |  |
| Lattice parameters | a = 5.03 Å b = 6.95 Å c = 4.52 Å | α = 90° β = 90° γ = 90° |  |  |  |  |
| Atomic Coordinates | Wyckoff site | x | y | z | Overall B | Occupation |
| Cr1 | 4c | 0.0425 | 1/4 | 0.8396 | 0 | 1.0 |
| Mn1 | 8d | 0.1919 | 0.0737 | 0.3446 |  | 1.0 |
| C1 | 4c | 0.8686 | 1/4 | 0.4562 |  | 1.0 |
| C2 | 4a | 0 | 0 | 0 |  | 0.25 |
| MSLS - Model A |
| Space group | Pnma (nr. 62) |  |  |  |  |  |
| Lattice parameters | a(O) = 5.09 Å b(O) = 6.98 Å c(O) = 4.55 Å | α = 90° β = 90° γ = 90° |  |  |  |  |
| Atomic Coordinates | Wyckoff site | x | y | z | B | Occupation |
| Cr1 | 4c | 0.0671 (4) | 1/4 | 0.8255 (3) | 0.065(10) | 1.0 |
| Mn1 | 8d | 0.1991 (5) | 0.0897 (3) | 0.3447 (2) | 0.116(5) | 1.0 |
| C1 | 4c | 0.823 (3) | 1/4 | 0.4648 (13) | 0.42(10) | 1.0 |
| C2 | 4a | 0 | 0 | 0 | 0.1 | 0.238(7) |

| DFT - Model B |
| --- |
| Space group | Pnma (nr. 62) |  |  |  |  |  |
| Lattice parameters | a = 5.07 Å b = 6.77 Å c = 4.56 Å | α = 90° β = 90° γ = 90° |  |  |  |  |
| Atomic Coordinates | Wyckoff site | x | y | z | Overall B | Occupation |
| Mn1 | 4c | 0.0425 | 1/4 | 0.8396 | 0 | 1.0 |
| Mn2 | 8d | 0.1919 | 0.0737 | 0.3446 |  | 0.5 |
| Cr1 | 8d | 0.1919 | 0.0737 | 0.3446 |  | 0.5 |
| C1 | 4c | 0.8686 | 1/4 | 0.4562 |  | 1.0 |
| C2 | 4a | 0 | 0 | 0 |  | 0.25 |
| MSLS - Model B |
| Space group | Pnma (nr. 62) |  |  |  |  |  |
| Lattice parameters | a(O) = 5.09 Å b(O) = 6.98 Å c(O) = 4.55 Å | α = 90° β = 90° γ = 90° |  |  |  |  |
| Atomic Coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4c | 0.0688( 4) | 1/4 | 0.8289( 3) | 0.508(18) | 1.0 |
| Mn2 | 8d | 0.1945( 5) | 0.0914( 3) | 0.3468( 3) | 0.383( 7) | 0.5 |
| Cr1 | 8d | 0.1945( 5) | 0.0914( 3) | 0.3468( 3) | 0.383( 7) | 0.5 |
| C1 | 4c | 0.806( 3) | 1/4 | 0.4294(18) | 0.100000 | 0.63( 4) |
| C2 | 4a | 0 | 0 | 0 | 0.100000 | 0.062( 8) |

| DFT - Model C |
| --- |
| Space group | Pnma (nr. 62) |  |  |  |  |  |
| Lattice parameters | a = 5.03 Å b = 6.95 Å c = 4.52 Å | α = 90° β = 90° γ = 90° |  |  |  |  |
| Atomic Coordinates | Wyckoff site | x | y | z | Overall B | Occupation |
| Mn1 | 4c | 0.0425 | 1/4 | 0.8396 | 0 | 0.6666667 |
| Cr1 | 4c | 0.0425 | 1/4 | 0.8396 |  | 0.3333333 |
| Mn2 | 8d | 0.1919 | 0.0737 | 0.3446 |  | 0.6666667 |
| Cr2 | 8d | 0.1919 | 0.0737 | 0.3446 |  | 0.3333333 |
| C1 | 4c | 0.8686 | 1/4 | 0.4562 |  | 1.0 |
| C2 | 4a | 0 | 0 | 0 |  | 0.25 |
| MSLS - Model C |
| Space group | Pnma (nr. 62) |  |  |  |  |  |
| Lattice parameters | a(O) = 5.09 Å b(O) = 6.98 Å c(O) = 4.55 Å | α = 90° β = 90° γ = 90° |  |  |  |  |
| Atomic Coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4c | 0.0711( 4) | 1/4 | 0.8274( 3) | 0.683(17) | 0.6666667 |
| Cr1 | 4c | 0.0711( 4) | 1/4 | 0.8274( 3) | 0.683(17) | 0.3333333 |
| Mn2 | 8d | 0.1965( 5) | 0.0924( 3) | 0.3473( 2) | 0.386( 7) | 0.6666667 |
| Cr2 | 8d | 0.1965( 5) | 0.0924( 3) | 0.3473( 2) | 0.386( 7) | 0.3333333 |
| C1 | 4c | 0.810( 3) | 1/4 | 0.4571(17) | 0.1 | 0.796( 4) |
| C2 | 4a | 0 | 0 | 0 | 0.1 | 0.108( 8) |

Table S.9: Comparison of experimental crystal structure information of the M-carbide with DFT Models A, B and C.

| DFT – Model A |
| --- |
| Space group | P21/c (nr. 14) |  |  |  |  |  |
| Lattice parameters | a = 7.12 Å b = 4.57 Å c = 5.06 Å | α = 90.0° β = 91.4° γ = 90.0° |  |  |  |  |
| Atomic coordinates | Wyckoff site | x | y | z | Overall B | Occupation |
| Mn1 | 4e | 0.0993 | 0.3366 | 0.1767 | 0 | 0.75 |
| Cr1 | 4e | 0.0993 | 0.3366 | 0.1767 |  | 0.25 |
| Mn2 | 4e | 0.4500 | 0.3485 | 0.1886 |  | 0.75 |
| Cr2 | 4e | 0.4500 | 0.3485 | 0.1886 |  | 0.25 |
| Cr3 | 4e | 0.2548 | 0.8398 | 0.0397 |  | 1.0 |
| C1 | 4e | 0.2918 | 0.4372 | 0.8806 |  | 1.0 |
| C2 | 2a | 0 | 0 | 0 |  | 1.0 |
| MSLS – Model A |
| Space group | P21/c (nr. 14) |  |  |  |  |  |
| Lattice parameters | a(M) = 6.83 Å b(M) = 4.54 Å c(M) = 5.00 Å | α = 90.0° β(M) = 92.2° γ = 90.0° |  |  |  |  |
| Atomic coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4e | 0.102( 3) | 0.3194( 9) | 0.1334(14) | 0.1 | 0.75 |
| Cr1 | 4e | 0.102( 3) | 0.3194( 9) | 0.1334(14) | 0.1 | 0.25 |
| Mn2 | 4e | 0.430( 3) | 0.3742( 6) | 0.1528(17) | 0.71( 7) | 0.75 |
| Cr2 | 4e | 0.430( 3) | 0.3742( 6) | 0.1528(17) | 0.71( 7) | 0.25 |
| Cr3 | 4e | 0.2414(10) | 0.8573( 7) | 0.0091(15) | 0.81( 7) | 1.0 |
| C1 | 4e | 0.299( 2) | 0.4423(16) | 0.884( 2) | 3.2( 4) | 1.0 |
| C2 | 2a | 0 | 0 | 0 | 0.1 | 1.0 |

| DFT – Model B |
| --- |
| Space group | P21/c (nr. 14) |  |  |  |  |  |
| Lattice parameters | a = 7.13 Å b = 4.60 Å c = 5.07 Å | α = 90.0° β = 91.2° γ = 90.0° |  |  |  |  |
| Atomic coordinates | Wyckoff site | x | y | z | Overall B | Occupation |
| Mn1 | 4e | 0.1074 | 0.3235 | 0.1813 | 0 | 0.5 |
| Cr1 | 4e | 0.1074 | 0.3235 | 0.1813 |  | 0.5 |
| Mn2 | 4e | 0.4496 | 0.3495 | 0.1846 |  | 0.5 |
| Cr2 | 4e | 0.4496 | 0.3495 | 0.1846 |  | 0.5 |
| Mn3 | 4e | 0.2539 | 0.8325 | 0.0429 |  | 0.5 |
| Cr3 | 4e | 0.2539 | 0.8325 | 0.0429 |  | 0.5 |
| C1 | 4e | 0.2878 | 0.4422 | 0.8793 |  | 1.0 |
| C2 | 2a | 0 | 0 | 0 |  | 1.0 |
| MSLS – Model B |
| Space group | P21/c (nr. 14) |  |  |  |  |  |
| Lattice parameters | a(M) = 6.83 Å b(M) = 4.54 Å c(M) = 5.00 Å | α = 90.0° β(M) = 92.2° γ = 90.0° |  |  |  |  |
| Atomic coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4e | 0.103( 2) | 0.3220( 7) | 0.1327(13) | 0.1 | 0.5 |
| Cr1 | 4e | 0.103( 2) | 0.3220( 7) | 0.1327(13) | 0.1 | 0.5 |
| Mn2 | 4e | 0.4311(16) | 0.3731( 5) | 0.1534(13) | 0.19( 5) | 0.5 |
| Cr2 | 4e | 0.4311(16) | 0.3731( 5) | 0.1534(13) | 0.19( 5) | 0.5 |
| Mn3 | 4e | 0.2533( 8) | 0.8539( 6) | 0.0160(12) | 0.50( 4) | 0.5 |
| Cr3 | 4e | 0.2533( 8) | 0.8539( 6) | 0.0160(12) | 0.50( 4) | 0.5 |
| C1 | 4e | 0.306( 2) | 0.4464(16) | 1.8( 2) | 0.887( 2) | 1.0 |
| C2 | 2a | 0 | 0 | 0 | 0.1 | 1.0 |

| DFT – Model C |
| --- |
| Space group | P21/c (nr. 14) |  |  |  |  |  |
| Lattice parameters | a = 7.07 Å b = 4.64 Å c = 5.12 Å | α = 90.0° β = 92.0° γ = 90.0° |  |  |  |  |
| Atomic coordinates | Wyckoff site | x | y | z | Overall B | Occupation |
| Mn1 | 4e | 0.1066 | 0.3170 | 0.1842 | 0 | 0.25 |
| Cr1 | 4e | 0.1066 | 0.3170 | 0.1842 |  | 0.75 |
| Mn2 | 4e | 0.4477 | 0.3517 | 0.1874 |  | 0.25 |
| Cr2 | 4e | 0.4477 | 0.3517 | 0.1874 |  | 0.75 |
| Mn3 | 4e | 0.2537 | 0.8322 | 0.0464 |  | 1.0 |
| C1 | 4e | 0.2829 | 0.4473 | 0.8811 |  | 1.0 |
| C2 | 2a | 0 | 0 | 0 |  | 1.0 |
| MSLS – Model C |
| Space group | P21/c (nr. 14) |  |  |  |  |  |
| Lattice parameters | a(M) = 6.83 Å b(M) = 4.54 Å c(M) = 5.00 Å | α = 90.0° β(M) = 92.2° γ = 90.0° |  |  |  |  |
| Atomic coordinates | Wyckoff site | x | y | z | B | Occupation |
| Mn1 | 4e | 0.106( 2) | 0.3274( 7) | 0.1348(11) | 0.1 | 0.25 |
| Cr1 | 4e | 0.106( 2) | 0.3274( 7) | 0.1348(11) | 0.1 | 0.75 |
| Mn2 | 4e | 0.4451(15) | 0.3722( 5) | 0.1619(13) | 0.1 | 0.25 |
| Cr2 | 4e | 0.4451(15) | 0.3722( 5) | 0.1619(13) | 0.1 | 0.75 |
| Mn3 | 4e | 0.2598( 9) | 0.8484( 6) | 0.0183(14) | 0.69( 4) | 1.0 |
| C1 | 4e | 0.288( 3) | 0.4527(20) | 0.882( 2) | 1.9( 2) | 1.0 |
| C2 | 2a | 0 | 0 | 0 | 0.1 | 1.0 |